## Slide 1: SOP
Details for scaling up production

## Slide 2: Overview
(Insert overview illustration here)

## Slide 3: Metal Deposition
Si clean substrate, sputter Cr – Au – Cu
  Cr ~ 10 nm (0.8 nm/s)
  Au ~ 10 nm (1.5 nm/s)
  Cu ~ 10 nm?? (?? nm/s)
Spin-coat PMMA (thickness ~1-2 µm)
  Static spin-coating PMMA 950 A11 4000 rpm (spin curve 2 µm)

## Slide 4: Substrate Preparation
Use silicon wafer directly from packaging
  Do no wash or blow with N2 gun as they are already clean enough
Bake Si at 120 °C for 120 s
Spin coat PMMA 950 A10 at 4000 rpm for 1 min
Soft bake at 120 °C for 120 s

## Slide 5: Proton Beam Writing + Development
Dosage 100 – 150 nC/mm2
  Scan 2 x 50 – 75 nC/mm2 to even out any possible beam fluctuations
  Enable slits at accelerator side only after beam is more stable (~6 h)
Writing strategy: Stage scanning
  Beam scanning causes skewing, not perpendicular grid lines
Develop in IPA : DI = 7 : 3 until exposed areas are washed away
  Cannot be washed for too long; may overdevelop and cause rough sides
  Develop in intervals of 30 s – 1 min

## Slide 6: Pd Plating + Lift-off
Plate Pd at E6 Nanofab Lab clean room (~100 nm)
Soak sample into acetone
  Recent samples needed at least 30 min of acetone swirl (no pre-wash, used directly from pack, PMMA adhesion on Si good)
  One sample needed collectively 1 h of acetone swirl + 5 min ultrasonicate as a last resort (pre-washed, PMMA adhesion on Si not good)
  Check periodically

## Slide 7: Mask Preparation Steps for Micro Structures
Background
Quartz glass, 25 nm Cr layer enough to block UV (220 – 250 nm) [1]
Steps
Spin-coat AZ1518 on quartz glass (2000 rpm, 1 min static)
Draw pattern using laser writer
Develop using AZ400K : DI = 1 : 4
Sputter 25 nm Cr (~32 s, 0.8 nm/s)
Wash away remaining AZ1518 with acetone + ultrasonicator
[1] F. Zhang et al. Fabrication of free standing resolution standards using proton beam writing (2007)

## Slide 8: Micro Structures Lithography